TUGAS I

Tugas : contoh 2 divais & proses dari beberapa alternatif yang ada.

___________

Title		SSUPREM 3 Example 1. NMOS Silicon Gate

Comment	Gate Region

$		File s3ex1b

Comment	Initialize silicon substrate

Initilaixe	Structure=s3e1as

Comment	Implant Arsenic for source/drain regions

Implant		Arsenic	Dose=5E15	Energy=150

Comment	Drive-in Arsenic and re-oxidize source/drain regions

Diffusion	Temperature=1000	Time=30	DryO2

Comment	Deposit Phosphorus doped SiO2 using CVD

Deposit		Oxide	Thickness=.7500	Phosphorus Concentration=1.E21

Comment	Increase the diffusivity of phosphorus in oxide by two order of magnitude

Phosphorus	Oxide	Dix.0=4.56E7

Comment	Reflow glass to smooth surface and dops contact holes.

Diffusion	Temperature=1000	Time=30

Comment	Reopen contact holes.

Etch		Oxide

Comment	Deposit Aluminum

Deposit		Aluminum	Thickness=1.2	Spaces=10

Comment	Plot the chemical impurity distributions at this point

Print		Layer

Plot		Chemical Boron		Xmax=2.5	Clear	Axis	Linetype=2

+		title=Example-1b

Plot		Chemical Arsenic		Xmax=2.5	^Clear	^Axis	Linetype=3

Plot		Chemical Phosphorus	Xmax=2.5	^Clear	^Axis	Linetype=6

Plot		Chemical Net		Xmax=2.5	^Clear	^Axis

Comment	Save the structure.

Save		Structure	File=s3e1bs

Stop		End of SSUPREM 3 Example 1.

Title		SSUPREM 3 Example 2. Bipolar Ploy doped emitter.

$		Initial active region formation.

$		File s3ex2a

Comment	Initialize silicon substrate

Initialize	<100> Silicon, Boron 	Concentration=5e14

+		Thickness=5.	dX=.01	XdX=.05	Spaces=100

Comment	Grow masking oxide for non-active regions.

Diffusion	Temperature=1150 Time=100 WetO2

Comment	Etch the oxide over the buried layer regions.

Etch		Oxide

Comment	Implant and drive-in the antimony buried layer.

Implant		Antimony	Dose=5E14	Energy=120

Diffusion	Temperature=1150	Time=15	DryO2

Diffusion	Temperature=1150	Time=300

Print		Layer

Plot		Net	Chemical	Xmax=5

+			title=Example-2a1

Comment	Etch off the oxide

Etch		Oxide

Comment	Grow 1.6 micron	of arsenic doped epi.

Epitaxy		Temperature=1050	Time=4	Growth.Rate=.4

+		Arsenic	Gas.Conc=5E15

Comment	Grow a 400A pad oxide.

Diffusion	Temperature=1060	time=20	DryO2

Comment	Deposit	nitride to mask the field oxidation.

Deposit	Nitride	Thickness=.08

Comment	Plot the chemical impurity distributions at this point

Print		Layer

Plot		Chemical Boron		Xmax=5		Clear	Axis	Linetype=2

+		title=Example-2a2

Plot		Chemical Arsenic		Xmax=5		^Clear	^Axis	Linetype=4

Plot		Chemical Antimony	Xmax=5		^Clear	^Axis	Linetype=5

Plot		Chemical Net		Xmax=5		^Clear	^Axis

Comment	Save the simulation structure at this point for use in subsequent processing.

Savefile		Structure	File=s3e2as

Stop

Listing file untuk mencari DOPING PROFILE DIODA dengan PISCES2B

************************************************************

Date and time = 15-JAN-92 19:21:14

1... Title  PN diode transient simulation

2... $ Grid of the structure and doping distribution

3... $ SILVACO International 1991

4... mesh       rect  nx=100 ny=10  smooth=1 diag.flip

5... x.m        n=1   l=0.0  r=1.0

6... x.m        n=100  l=10500.0  r=1.0

7... y.m        n=1   l=0.0  r=1.0

8... y.m        n=10  l=8.0  r=1.0

9... $ Regions and Electrodes

10... region     num=1 silicon

11... elec       num=1 x.min=0.0 length=999.0

12... elec       num=2 bottom

13... $ Doping profile

14... doping     uniform conc=1.2e15 n.type  outf=dd1dio

15... doping     gauss   conc=1.2e17 p.type junc=0.922 x.r=10000.0  ratio=0.7

16... regrid     doping ratio=4 log smooth.k=1                 dopfile=dd1dio

17... regrid     doping ratio=4 log smooth.k=1 outf=mesh.dd1  dopfile=dd1dio

18... $

19... plot.1d    x.s=0.0 x.e=5.0 y.s=0.0 y.e=0.0 doping abs log pa

20... plot.1d    x.s=1.0 x.e=1.0 y.s=0.0 y.e=5.0 doping abs log pa

21... plot.2d    x.min=9950 x.max=10000 grid boundary no.top no.fill  pa

22... plot.2d    x/min=9950 x.max=10000 junction boundary l.elect=2 l.bound=3 l.junct=6 no.fill pa

23... end

*****************************

PN diode transient simulation

*****************************

Mesh statistics :

Total grid points =  1000

Total no. of triangles =  1782

Obtuse triangles =    0  ( 0.0%)

Mesh statistics :

Total grid points =  1385

Total no. of triangles =  2550

Obtuse triangles =    1332  ( 52.2%)

Mesh statistics :

Total grid points =  2430

Total no. of triangles = 4545

Obtuse triangles =   2182  ( 48.0%)

Grid written to mesh.dd1

Output :

1. Dioda

2. BJT transistor :